## Slide 1
OPTICAL AND ELECTRICAL PROPERTIES OF ZnTe AND ZnTe:O THIN FILMS DEPOSITED BY CSVT TECHNIQUE
M. A. González Trujillo1, M.L. Albor Aguilera2, D.A. Rodríguez Morán3 ,Y. Matsumoto Kuwabara4 , M. Galván Arellano4, A. Morales Acevedo4, G. Casados Cruz4
1ESCOM – IPN, Formación Básica, U.P.A.L.M., Zacatenco, México D.F., 07738, México.
2ESFM-IPN, Depto. Física, U.P.A.L.M., Zacatenco, México D.F. 07738, México.
3ESIQIE-IPN, Depto. Ing. Química Industrial, U.P.A.L.M., Zacatenco, México D.F., 07738, México.
4CINVESTAV-SEES-IPN, Av. IPN 2508, Zacatenco, México D.F. 07360, México.
EXPERIMENT
ABSTRAC
a
b
c
Zinc Telluride (ZnTe) thin films were deposited onto glass and CdTe substrates by CSVT (Close Space Vapor Transport) technique. The analysis of the chemical compositions for the as-deposited as well as annealed ZnTe thin films was estimated by using the method of energy dispersive analysis of x-ray (EDAX). The morphological structural, optical and electrical properties were studied.
Sample a deposited on SnO2:F
Sample c deposited on glass
Sample b deposited on SnO2:F
Sample d deposited on glass
Sample e deposited on CdS
Sample f deposited on glass
Pessure: 100 mTorr (100% O2)
Pessure: 100 mTorr (100% Ar)
Pessure: 100 mTorr (100% O2)
CdTe Deposit
Tf=630°C
Ts=530°C
Deposition time= 3 min
Pressure: 100 mTorr; (50º% O2 and 50% Ar)
ZnTe Deposite
Tf=550°C
Ts=--- °C
Deposition time= 3 min
Development
experimental
Figure 3. SEM images, 10 KV. Samples CdTe: a), c) and e) deposited at T1=630°C and T2=530°C. Samples CdTe/ZnTe were deposited at T1=630°C and T2=530°C, doped at T3=550°C: b) and d) on O2 atmosphere and f) on Ar atmosphere
Sample | EDAX |  |  | Thickness (µm) | Sheet resistance (Ω/ □ ) | Resistivity (Ω•m)
 | % Te | % Cd | % Zn |  |  | 
a) | 48.71 | 51.29 | --- | 7.3 | -- | --
b) | 57.29 | 42.51 | 0.41 | 8.5 | 47.40 x 103 | 1.2 x103
c) | 49.52 | 50.48 | --- | 5.6 | --- | --
d) | 57.09 | 42.76 | 0.15 | 6.9 | 81.25 x 103 | 1.3 x103
e) | 46.13 | 53.87 | -- | 18 | -- | --
f) | 56.76 | 43.24 | -- | 4.6 | 20.983 x 103 | 8.7 x102
RESULTS
Figure 1.Evaporation Chamber consists of a: a) block of substrate, b)block of source and c) graphite furnace
Figure 2. Evaporation Chamber for the ZnTe
The deposition temperatures used for the samples were 530 °C and 630°C for the source (T1) and substrate (T2) respectively (fig. 1), under the following conditions: 0.1 Torr, controlled atmosphere (50% O2 and 50% Ar). 0,013 g was placed in a boat CdTe with three divisions , this was for three minutes. The CdTe samples were doped whit ZnTe using a source temperature of 550 °C on controlated atmosphere of O2 and Ar.
Figure 4. X-R spectra of (a),(c),(e) CdTe as grown; (b),(d) CdTe with ZnTe on diferent substrats
REFERENCES
[1] M.L. Albor Aguilera y M. A. González Trujillo, Tesis de Licenciatura “Construcción de un Sistema de Crecimiento de Películas Delgadas Semiconductoras por la Técnica GREG", 1993.
[2] M. Tufiño Velázquez, G. Contreras Puente, M.L. Albor Aguilera, M.A. González Trujillo, A.D. Compaan, Revista Mexicana de Física 44(6) (1998) 589-595.
[3] A. Romeo, R. Wendt, et al, “Development of efficient and stable back contacs on CdTe/CdS solar cells” Thin solid films (2001).
[4] M. S. Hossain, R. Islam Et al, “Structural, elemental compositions and optical properties of ZnTe:V thin films”. Chalcogenide Letters Vol. 7, 2010.
[5]Dieter K. “Semiconductor material and device characterization” second edition, a Wiley-Interscience Publication, Canada, 1998
● Electrical measurements reveals a CdTe conductivity is improved with Te.
● A p+ región was created with ZnTe.
● Crystalline quality is reduced by CdTe films with ZnTe. (annalysis of X-R and photoacustic spectra).
● The properties obtained with ZnTe how back contact can be use on photovoltaic dispositive.
CONCLUSIONS
a)
b)
c)
d)
e)
f)
Table 1. Comparative chemical quantification, electric properties of CdTe and ZnTe/CdTe thin films.
Figure 7. Photoacoustic spectra of CdTe and ZnTe/CdTe